μ-reactors for Heterogeneous Catalysis

---
Outline
- Motivation & Introduction
- Heating
- The Grand Master Plan
- Area Measurements
- Oscillating CO oxidation
- Sensitivity Measurements
- Time-Of-Flight Mass Spectrometry
- Summary

---
Introduction & Motivation
Heterogeneous catalysis is important
in many parts of modern life:
Fertilizers
Crude oil cleaning
Chemical industry
Car exhaust cleaning
…
Harvesting of solar energy
Chemical processes utilizing excess energy from renewable sources
Energy storage

---
Introduction & Motivation
Many kinds of experimental catalysts needs to be tested in an early state of development
Often the amount of material will be extremely limited due to factors such as
Material costs
Fabrication constraints
Toxicity

---
Introduction & Motivation
The μ-reactor provides an excellent platform for testing of experimental catalysts.
Advantages includes:
High sensitivity
Low gas consumption
High safety level
Low thermal mass
Photo: Thomas Pedersen
CAD-drawing: Thomas Pedersen

---
Experimental Setup
Photo: Mathias Kjærgaard Christensen

---
Experimental Setup
Photo: Mathias Kjærgaard Christensen

---
Experimental Setup

---
A Typical Measurement
CO oxidation on Pd thin film

---
General Measurement Strategy

---
General Measurement Strategy
The Grand Master Plan:
Thin-film measurements
Nanoparticle measurements
Publish

---
Heating

---
Heating

---
Temperature profiles

---
Heating V2.0
CAD Drawing: Thomas Pedersen
Photo: Mathias Kjærgaard Christensen

---
Measuring surface area

---
Measuring surface area
We need a way of measuring the active area of the catalysts in the reactor

---
Area Measurements
Measurement principle:
CO-titration
Dose oxygen
Evacuate reactor
Dose CO
Watch for CO2
Limitations
Works only for Pt
Not very sensitive

---
Area Measurements
Calibration experiments performed on thin films
Easy cleaning
Known surface area
Stable system allows for lots of experimentation

---
Area Measurements
Measurement program:
Heating to 420◦ C in 1.0 bar O2
Heating to 300◦ C in 1.0 bar He
Heating to 300◦ C in 0.5 bar CO
Heating to 350◦ C in 1.0 bar O2
Heating to 300◦ C in 0.5 bar CO
Heating to 250◦ C in 1.0 bar O2
Heating to 300◦ C in 0.5 bar CO
Heating to 150◦ C in 1.0 bar O2
Heating to 300◦ C in 0.5 bar CO
According to the Grand Master Plan, we should now measure on nanoparticles.
The chosen sample has a nominal coverage of 10% of 5nm particles.
Structural modiﬁcation of Pt model systems under high pressure CO annealing
D.N. McCarthy, et. al C.E. Strebel, T.P. Johansson, A. den Dunnen, A. Nierhoff, J.H.Nielsen, and Ib Chorkendorff, 2012

---
Area Measurements
Nanoparticle sample
Thin-film sample

---
Area Measurements

---
Area Measurements

---
Area Measurements
The Grand Master Plan:
Thin-film measurements
Nanoparticle measurements
Publish
Establish new characterization tool for the reactors

---
Oscillating Reactions

---
Oscillating Reactions
The story starts a dark and stormy saturday evening....
Experiments for a bachelors thesis1 a was done and the setup was idling for the rest of the weekend
An idling sample of size-selected nano-clusters is the perfect time for random experiments!
Tried to run a classic CO oxidation light-off experiment in extremely high oxygen concentration
1 Mikkel Rykær Kraglund: Reactivity of mass selected nanoparticles measured in microreactors, 2011

---
Oscillating Reactions
Data with unusually low quality called for an explanation

---
Oscillating Reactions

---
Oscillating Reactions
A more systematic study was initialized
A large set of nanoparticle samples was tested for oscillatory behavior

---
Oscillating Reactions
Model based on work from:
B. L. M. Hendriksen, M. D. Ackermann, R. van Rijn, D. Stoltz, I. Popa, O. Balmes, A. Resta, D. Wermeille, R. Felici, S. Ferrer, and J. W.
M. Frenken. The role of steps in surface catalysis and reaction oscillations. Nature Chemistry, 2(9):730–734, September 2010.

---
Oscillating Reactions
Oscillations self sustained for several days, with steadily increasing period.

---
Oscillating Reactions
Oscillations are heavily dependent on temperature and mildly dependent on gas composition.

---
Oscillating Reactions
The Grand Master Plan:
Thin film measurements
Nanoparticle measurements
Publish Submit

---
Sensitivity Measurements
Observation. The sample loading for the oscillation experiments was very low.
Question. How small amounts of catalyst can be measured in the μ-reactor setup?

---
Sensitivity Measurements
Thomas Pedersen produced a wafer with Pt spots of different sizes. Six of these have so far been successfully measured.
#	Radius / μm	Area / μm2	Reactor coverage
N5	3.5	38.5	4.9 x 10-7
N8	15	707	9.0 x 10-6
N9	25	1960	2.5 x 10-5
N10	50	7850	1.0 x 10-4
N11	250	196000	2.5 x 10-3

---
Sensitivity Measurements
#	Radius / μm	Area / μm2	Reactor coverage
N5	3.5	38.5	4.9 x 10-7
N8	15	707	9.0 x 10-6
N9	25	1960	2.5 x 10-5
N10	50	7850	1.0 x 10-4
N11	250	196000	2.5 x 10-3

---
Sensitivity Measurements
Background correction
To do quantitative analysis, it is necessary to subtract the CO2 background.

---
Sensitivity Measurements
Background correction
To do quantitative analysis, it is necessary to subtract the CO2 background.
Background turns out to be dominated by oxygen:
ICO2 ~ 0.0082 x IO2

---
Sensitivity Measurements
Background correction
Using the background correction
the linear region can be significantly extended.

---
Sensitivity Measurements
Mass Spec Calibration
How do we get from MS-output to actual turn over frequency?
Use the approximately known total flow and calculate from the total SEM current.

---
Sensitivity Measurements
From the known sensitivity absolute turnover can be calculated.
Area normalization shows that all samples falls on approximately the same line.
Number of sites on Pt: ~6.5x106 μm-2

---
Sensitivity Measurements
Finally, we are able to calculate absolute numbers for activation energy and prefactor.
Errorbars expresses fitting uncertainty and thus under estimates the real error.

---
Sensitivity Measurements
Take home messages regarding sensitivity:
- CO oxidation can be extremely efficient on Pt
- Even minute amounts of metal (espcially Pt) contamination must be avoided in the μ-reactors
The Grand Master Plan:
Thin film measurements
Nanoparticle measurements
Publish

---
Time-Of-Flight Mass Spectrometry

---
Time-Of-Flight Mass Spectrometry
Drawing:
Jordan TOF Products, Inc
Drawing: Thomas Andersen

---
Time-Of-Flight Mass Spectrometry

---
Time-Of-Flight Mass Spectrometry
Mass resolution much superior to a QMS allows for separation of OH and NH3

---
Time-Of-Flight Mass
Spectrometry
The Grand Master Plan:
Thin film measurements
Nanoparticle measurements
Thin film measurements
Publish

---
Conclusions
The many advantages of the μ-reactor platform has been demonstrated
A new and improved heating scheme has been implemented
A method to determine the amount of actual active catalyst surface area has been developed (at least for Platinum...)
Oscillating CO oxidation reactions has been demonstrated
The very high sensitivity of the platform has been shown and turn over frequencies of almost 105 has been achived
The successful application of Time-Of-Flight Mass Spectrometry to the platform has been shown

---
Acknowledgments
Thank you to a long list of people...
My familly and friends (especially Sine and Gro & Sia!)
Ib Chorkendorff
Ole Hansen
Tine Klitmøller
Thomas Pedersen
Dan, Peder, Peter and Anders
Jane Hvolbæk Nielsen
Ole Trinhammer
Anders Nierhoff
Peter Vesborg
Mathias Kjærgaard Sørensen
Thomas Andersen
Kenneth Nielsen
+ everybody at CINF!!!